Concrete To accompany the Agricultural Education, Construction, and Engineering and Technology Curriculums

CTAE Resource Network, Instructional Resources Office, 2010

Georgia Performance Standards: ACT-C1-5. Students will know and understand the materials, processes, and safety related to all cement and concrete products. AG-AGC-6. Students will demonstrate concrete construction techniques to industry standards. ACT-M1-3. Students will become familiar with the selection, handling, storage, and proper use of masonry materials. See the end of this document for complete GPS listing

Student Information Guide

Directions:

Use the information in this student information sheet to complete the accompanying student study sheet. Complete all items on the study sheet and turn in to the teacher.

Concrete

Concrete is a construction material composed of cement (commonly Portland cement) as well as other cementitious materials such as fly ash and slag cement, aggregate (generally a coarse aggregate such as gravel, limestone, or granite, plus a fine aggregate such as sand), water, and chemical admixtures. The word concrete comes from the Latin word "concretus" (meaning compact or condensed), the past participle of "concresco", from "com-" (together) and "cresco" (to grow).

Concrete solidifies and hardens after mixing with water and placement due to a chemical process known as hydration. The water reacts with the cement, which bonds the other components together, eventually creating a stone-like material. Concrete is used to make pavements, pipe, architectural structures, foundations, motorways/roads, bridges/overpasses, parking structures, brick/block walls and footings for gates, fences and poles.

Concrete is used more than any other man-made material in the world. As of 2006, about 7.5 cubic kilometers of concrete are made each year—more than one cubic meter for every person on Earth. Concrete powers a US $35-billion industry which employs more than two million workers in the United States alone. More than 55,000 miles (89,000 km) of highways in the United States are paved with this material. Reinforced concrete and prestressed concrete are the most widely used modern kinds of concrete functional extensions.

History

Concrete has been used for construction in various ancient civilizations. An analysis of ancient Egyptian pyramids has shown that concrete was employed in their construction.

During the Roman Empire, Roman concrete (or Opus caementicium) was made from quicklime, pozzolanic ash/pozzolana, and an aggregate of pumice. Its widespread use in many Roman structures, a key event in the history of architecture termed the Concrete Revolution, freed Roman construction from the restrictions of stone and brick material and allowed for revolutionary new designs both in terms of structural complexity and dimension.

Modern tests show Opus caementicium to be as strong as modern Portland cement concrete in its compressive strength (ca. 200 kg/cm2).  However, due to the absence of reinforced steel, its tensile strength was far lower and its mode of application was also different:

The widespread use of concrete in many Roman structures has ensured that many survive to the present day. The Baths of Caracalla in Rome are just one example of the longevity of concrete, which allowed the Romans to build this and similar structures across the Roman Empire. Many Roman aqueducts and Roman bridges have masonry cladding to a concrete core, a technique they used in structures such as the Pantheon, the dome of which is concrete.

The secret of concrete was lost for 13 centuries until 1756, when the British engineer John Smeaton pioneered the use of hydraulic lime in concrete, using pebbles and powdered brick as aggregate. Portland cement was first used in concrete in the early 1840s. This version of history has been challenged however, as the Canal du Midi was constructed using concrete in 1670.

# Additives

Recently, the use of recycled materials as concrete ingredients is gaining popularity because of increasingly stringent environmental legislation. The most conspicuous of these is fly ash, a by-product of coal-fired power plants. This has a significant impact by reducing the amount of quarrying and landfill space required, and, as it acts as a cement replacement, reduces the amount of cement required to produce a solid concrete.

Concrete additives have been used since Roman and Egyptian times, when it was discovered that adding volcanic ash to the mix allowed it to set under water. Similarly, the Romans knew that adding horse hair made concrete less liable to crack while it hardened, and adding blood made it more frost-resistant.

In modern times, researchers have experimented with the addition of other materials to create concrete with improved properties, such as higher strength or electrical conductivity.

Composition

There are many types of concrete available, created by varying the proportions of the main ingredients below. By varying the proportions of materials, or by substitution for the cemetitious and aggregate phases, the finished product can be tailored to its application with varying strength, density, or chemical and thermal resistance properties.

The mix design depends on the type of structure being built, how the concrete will be mixed and delivered, and how it will be placed to form this structure.

# Cement

Portland cement is the most common type of cement in general usage. It is a basic ingredient of concrete, mortar, and plaster. English masonry worker Joseph Aspdin patented Portland cement in 1824; it was named because of its similarity in color to Portland limestone, quarried from the English Isle of Portland and used extensively in London architecture. It consists of a mixture of oxides of calcium, silicon and aluminum. Portland cement and similar materials are made by heating limestone (a source of calcium) with clay, and grinding this product (called clinker) with a source of sulfate (most commonly gypsum). The manufacture of Portland cement creates about 5 percent of human CO2 emissions.

Water

Combining water with a cementitious material forms a cement paste by the process of hydration. The cement paste glues the aggregate together, fills voids within it, and allows it to flow more freely.

Less water in the cement paste will yield a stronger, more durable concrete; more water will give an freer-flowing concrete with a higher slump.

Impure water used to make concrete can cause problems when setting or in causing premature failure of the structure.

Hydration involves many different reactions, often occurring at the same time. As the reactions proceed, the products of the cement hydration process gradually bond together the individual sand and gravel particles, and other components of the concrete, to form a solid mass.

# Aggregates

Fine and coarse aggregates make up the bulk of a concrete mixture. Sand, natural gravel and crushed stone are mainly used for this purpose. Recycled aggregates (from construction, demolition and excavation waste) are increasingly used as partial replacements of natural aggregates, while a number of manufactured aggregates, including air-cooled blast furnace slag and bottom ash are also permitted.

Decorative stones such as quartzite, small river stones or crushed glass are sometimes added to the surface of concrete for a decorative "exposed aggregate" finish, popular among landscape designers.

# Reinforcement

Concrete is strong in compression, as the aggregate efficiently carries the compression load. However, it is weak in tension as the cement holding the aggregate in place can crack, allowing the structure to fail. Reinforced concrete solves these problems by adding either steel reinforcing bars, steel fibers, glass fiber, or plastic fiber to carry tensile loads.

Concrete Production

The processes used vary dramatically, from hand tools to heavy industry, but result in the concrete being placed where it cures into a final form.

When initially mixed together, Portland cement and water rapidly form a gel, formed of tangled chains of interlocking crystals. These continue to react over time, with the initially fluid gel often aiding in placement by improving workability. As the concrete sets, the chains of crystals join up, and form a rigid structure, gluing the aggregate particles in place. During curing, more of the cement reacts with the residual water (hydration).

This curing process develops physical and chemical properties, including mechanical strength, low moisture permeability, and chemical and volumetric stability, among other qualities.

# Mixing concrete

Thorough mixing is essential for the production of uniform, high quality concrete. Therefore, equipment and methods should be capable of effectively mixing concrete materials containing the largest specified aggregate to produce uniform mixtures of the lowest slump practical for the work. Separate paste mixing has shown that the mixing of cement and water into a paste before combining these materials with aggregates can increase the compressive strength of the resulting concrete. The paste is generally mixed in a high-speed, shear-type mixer at a w/cm (water to cement ratio) of 0.30 to 0.45 by mass. The cement paste premix may include admixtures such as accelerators or retarders, plasticizers, pigments, or silica fume. The latter is added to fill the gaps between the cement particles. This reduces the particle distance and leads to a higher final compressive strength and a higher water impermeability. The premixed paste is then blended with aggregates and any remaining batch water, and final mixing is completed in conventional concrete mixing equipment.

High-energy mixed concrete (HEM concrete) is produced by means of high-speed mixing of cement, water and sand with net specific energy consumption at least 5 kilojoules per kilogram of the mix. It is then added to a plasticizer admixture and mixed after that with aggregates in conventional concrete mixer. This paste can be used itself or foamed (expanded) for lightweight concrete. Sand effectively dissipates energy in this mixing process. HEM concrete fast hardens in ordinary and low temperature conditions, and possesses increased volume of gel, drastically reducing capillarity in solid and porous materials. It is recommended for precast concrete in order to reduce quantity of cement, as well as for concrete roof and siding tiles, paving stones and lightweight concrete block production.

The easiest way to add strength is to add cement. The factor that most predominantly influences concrete strength is the ratio of water to cement in the cement paste that binds the aggregates together. The higher this ratio is, the weaker the concrete will be and vice versa. Every desirable physical property that you can measure will be adversely effected by adding more water.

# Workability

Workability is the ability of a fresh (plastic) concrete mix to fill the form/mold properly with the desired work (vibration) and without reducing the concrete's quality. Workability depends on water content, aggregate (shape and size distribution), cementitious content and age (level of hydration), and can be modified by adding chemical admixtures. Raising the water content or adding chemical admixtures will increase concrete workability. Excessive water will lead to increased bleeding (surface water) and/or segregation of aggregates (when the cement and aggregates start to separate), with the resulting concrete having reduced quality. The use of an aggregate with an undesirable gradation can result in a very harsh mix design with a very low slump, which cannot be readily made more workable by addition of reasonable amounts of water.

Workability can be measured by the concrete slump test, a simplistic measure of the plasticity of a fresh batch of concrete following the ASTM C 143 or EN 12350-2 test standards. Slump is normally measured by filling an "Abrams cone" with a sample from a fresh batch of concrete. The cone is placed with the wide end down onto a level, non-absorptive surface. It is then filled in three layers of equal volume, with each layer being tamped with a steel rod in order to consolidate the layer. When the cone is carefully lifted off, the enclosed material will slump a certain amount due to gravity. A relatively dry sample will slump very little, having a slump value of one or two inches (25 or 50 mm). A relatively wet concrete sample may slump as much as eight inches.

High-flow concrete, like self-consolidating concrete, is tested by other flow-measuring methods. One of these methods includes placing the cone on the narrow end and observing how the mix flows through the cone while it is gradually lifted.

After mixing, concrete is a fluid and can be pumped to where it is needed.

# Curing

In all but the least critical applications, care needs to be taken to properly cure concrete, and achieve best strength and hardness. This happens after the concrete has been placed. Cement requires a moist, controlled environment to gain strength and harden fully. The cement paste hardens over time, initially setting and becoming rigid though very weak, and gaining in strength in the days and weeks following. In around 3 weeks, over 90% of the final strength is typically reached, though it may continue to strengthen for decades.

Hydration and hardening of concrete during the first three days is critical. Abnormally fast drying and shrinkage due to factors such as evaporation from wind during placement may lead to increased tensile stresses at a time when it has not yet gained significant strength, resulting in greater shrinkage cracking. The early strength of the concrete can be increased by keeping it damp for a longer period during the curing process. Minimizing stress prior to curing minimizes cracking. High early-strength concrete is designed to hydrate faster, often by increased use of cement which increases shrinkage and cracking.

During this period concrete needs to be in conditions with a controlled temperature and humid atmosphere. In practice, this is achieved by spraying or ponding the concrete surface with water, thereby protecting concrete mass from ill effects of ambient conditions.

Properly curing concrete leads to increased strength and lower permeability, and avoids cracking where the surface dries out prematurely. Care must also be taken to avoid freezing, or overheating due to the exothermic setting of cement (the Hoover Dam used pipes carrying coolant during setting to avoid damaging overheating). Improper curing can cause scaling, reduced strength, poor abrasion resistance and cracking.

Environmental Impact

# Worldwide CO2 emissions and global change

The cement industry is one of two primary producers of carbon dioxide (CO2), creating up to 5 percent of worldwide emissions of this gas. The embodied carbon dioxide (ECO2) of a ton of concrete varies with mix design and is in the range of: 75–176 kg CO2/ton 0.075 - 0.176 ton CO2/ton. Cement manufacture contributes greenhouse gases both directly through the production of carbon dioxide when calcium carbonate is heated, producing lime and carbon dioxide, and also indirectly through the use of energy, particularly if the energy is sourced from fossil fuels. The cement industry produces 5% of global man-made CO2 emissions, of which 50 % is from the chemical process, and 40 % from burning fuel.

# Surface runoff

Surface runoff, when water runs off impervious surfaces, such as non-porous concrete, can cause heavy soil erosion. Urban runoff tends to pick up gasoline, motor oil, heavy metals, trash and other pollutants from sidewalks, roadways and parking lots. The impervious cover in a typical city sewer system prevents groundwater percolation five times more than that of a typical woodland of the same size. A 2008 report by the United States National Research Council identified urban runoff as a leading source of water quality problems.

# Urban heat

Both concrete and asphalt are the primary contributors to what is known as the urban heat island effect.

Using light-colored concrete has proven effective in reflecting up to 50% more light than asphalt and reducing ambient temperature. A low albedo value, characteristic of black asphalt, absorbs a large percentage of solar heat and contributes to the warming of cities. By paving with light colored concrete, in addition to replacing asphalt with light-colored concrete, communities can lower their average temperature.

Many U.S. cities show that pavement comprise approximately 30-40% of their surface area. This directly impacts the temperature of the city, as demonstrated by the urban heat island effect. In addition to decreasing the overall temperature of parking lots and large paved areas by paving with light-colored concrete, there are supplemental benefits. One example is 10-30% improved nighttime visibility. The potential of energy saving within an area is also high. With lower temperatures, the demand for air conditioning decreases, saving vast amounts of energy.

Atlanta has tried to mitigate the heat-island effect. City officials noted that when using heat-reflecting concrete, their average city temperature decreased by 6 °F. New York City offers another example. The Design Trust for Public Space in New York City found that by slightly raising the albedo value in their city, beneficial effects such as energy savings could be achieved. It was concluded that this could be accomplished by the replacement of black asphalt with light-colored concrete.

# Concrete dust

Building demolition and natural disasters such as earthquakes often release a large amount of concrete dust into the local atmosphere. Concrete dust was concluded to be the major source of dangerous air pollution following the Great Hanshin earthquake.

Health and Safety

The presence of some substances in concrete, including useful and unwanted additives, can cause health concerns. Natural radioactive elements (K, U and Th) can be present in various concentration in concrete dwellings, depending on the source of the raw materials used. Toxic substances may also be added to the mixture for making concrete by unscrupulous makers. Dust from rubble or broken concrete upon demolition or crumbling may cause serious health concerns depending also on what had been incorporated in the concrete.

# Concrete handling/safety precautions

Handling of wet concrete must always be done with proper protective equipment. Contact with wet concrete can cause skin burns due to the caustic nature of the mixture of cement and water.

Georgia Performance Standards

ACT-C1-5.  Students will know and understand the materials, processes, and safety related to all cement and concrete products.

a. Demonstrate knowledge of the safety procedures associated with construction and use of concrete products.

b. Demonstrate knowledge of properties and composition of concrete products.

AG-AGC-6.  Students will demonstrate concrete construction techniques to industry standards.

ACT-M1-3.  Students will become familiar with the selection, handling, storage, and proper use of masonry materials.

a. Demonstrate the correct use of different types of materials used in the masonry trade, including mortar, admixtures, brick                         and block.

License & Verification

Text is available under the Creative Commons Attribution-ShareAlike License; additional terms may apply. See Terms of Use for details. - http://creativecommons.org/licenses/by-sa/3.0/

Wikipedia® is a registered trademark of the Wikimedia Foundation, Inc., a non-profit organization.

This document, originally from Wikipedia, has been modified
and the information has been independently verified.

# Text boxes

CONCRETE

Concrete Blocks

Opus caementicium laying bare on a tomb near Rome. In contrast to modern concrete structures, the concrete walls of Roman buildings were covered, usually with brick or stone.

Cement and sand ready to be mixed.

Installing rebar in a floor slab during a concrete pour

A concrete slab ponded while curing.

Cement being mixed with sand and water to form concrete.