## Module 02106-05
Plastic Pipe and Fittings

Lesson 1 of 2: Introduction to Plastic Pipe, and Plastic Pipe and Fittings

This lesson is a classroom session in which the students will learn about plastic pipe and plastic pipe fittings used in modern plumbing systems.  Students will identify types of plastic pipes and identify various plastic pipe fittings and valves to fulfill Performance Task requirements.

Objectives

Upon completion of this lesson, the student should be able to:

- Identify types of materials and schedules of plastic pipe.

- Describe the advantages and disadvantages of plastic pipes used in plumbing systems.

- Identify proper and improper applications of plastic pipe.

- Identify types of valves and fittings used with plastic pipe.

- Explain proper procedures for the handling, storage, and protection of plastic pipes.

Performance Requirements

  - Identify types of plastic pipes.  This corresponds to Performance Task 1.

  - Identify fittings and valves and their uses. This corresponds to Performance Task 2.

Reading Assignment

  - Module 02106, Sections 1 thru 3

Slide Presentation

  - Module 02106, Part 1 (Slides 1 thru 16)

Suggested Equipment/Materials

  - Samples of various types of plastic pipe and pipe fittings.

Suggested Student Activity

  - Have students visit a residential construction site.  Have them list all the applications they observe where plastic pipe is being used such as DWV systems, hot and cold water supply lines, irrigation or lawn sprinkler systems, AC condensate drains, etc.  This will enable students to get a feel for the widespread use of plastic pipe in new home construction.

Testing

  - Module Review Test Questions 1 thru 5 for Sections 1.0.0 - 2.0.0, and Questions 1 thru 7 for Sections 3.0.0. – 4.0.0.

  - CONTREN( Connect, Active Figures 1, 8 & 9

Suggested Lab Activity

  - Students must identify types of plastic pipe and identify fittings and valves and their usage.

Additional Resources

  - Plastic Piping Handbook, Weimar, TX, Culinary and Hospitality Industry Publications Services

  - www.plasticpipe.org (Plastic Pipe Institute) Information about plastic pipe applications.

  - Contren Connect Level 1Plumbng Annotated Instructors Guide (available from the NCCER)

SLIDE 1

  - Review the objectives for the module.

  - Review the objectives to be covered in this lesson.  Ask students if they have any questions about the lesson or course objectives.

SLIDE 2

  - Describe the advantages and disadvantages of using plastic pipe in plumbing systems.

  - Ask students of ways that these advantages and disadvantages might affect their job on a daily basis.  Example: Lighter weight of the pipe means they don’t have to lift as much, saving their backs.

SLIDE 3

  - Explain the differences between thermoplastic and thermosetting plastic pipe.

  - Explain the differences between solid wall and cellular core wall plastic pipes and the advantages and disadvantages of both types.

SLIDE 4

  - Explain how schedules and SDRs relate to wall thickness of plastic pipe.

  - Explain the relationship of outside diameter (OD) and wall thickness.

  - Have samples of Schedule 40 and Schedule 80 plastic pipe available to pass around the class.

SLIDE 5

  - Explain all aspects of plastic pipe labeling.

  - Provide students with samples of labeled plastic pipe and have them read the label.

SLIDE 6

  - Explain that the plastic pipe and fittings made by different manufacturers are not always compatible with each other.

  - Describe the six types of plastic pipes and their common applications.

  - Have a sample of each of the six types of plastic pipe available to pass around the class.

SLIDE 7

  - Describe the properties of ABS pipe and where it is typically used in a plumbing system.

  - Pass a sample of ABS pipe and an ABS fitting around the class.

SLIDE 8

  - Describe the properties of PVC pipe and where it is typically used in a plumbing system.

  - Pass a sample of PVC pipe and a PVC fitting around the class.

SLIDE 9

  - Describe the properties of CPVC pipe and where it is typically used in a plumbing system.

  - Pass a sample of CPVC pipe and a CPVC fitting around the class.

SLIDE 10

  - Describe the properties of PE pipe and where it is typically used in a plumbing system.

  - Pass a sample of PE pipe and a PE fitting around the class.

SLIDE 11

  - Describe the properties of PEX pipe and where it is typically used in a plumbing system.

  - Pass a sample of PEX pipe and a PEX fitting around the class.

SLIDE 12

  - Describe the properties of PB pipe and where it is typically used in a plumbing system.

  - Pass a sample of PB pipe and a PB fitting around the class.

  - Describe the problems associated with PB pipe and state that it is no longer being used.

  - Describe the procedures for storing and handling plastic pipe.

Have students answer Review Questions for Sections 1.0.0 - 2.0.0. Provide correct answers and remediation at the end of the quiz.

SLIDES 13 & 14

  - Explain that a pipe’s use determines what kinds of fittings and joints are needed.

  - Use Figure 8 (Slide 13) and Table 3 (Slide 14) to describe the various fittings and where they are typically used.

  - Have samples of various fittings available to pass around the class.

SLIDES 15 & 16

  - Explain what a DWV system is and some of its unique requirements.

  - Use Figure 9 (Slide 15) and Table 4 (Slide 16) to describe the various DWV fittings and where they are typically used.

  - Have samples of various DWV fittings available to pass around the class.

Have students answer Review Questions 1 thru 7 for Section 3.0.0 – 4.0.0. Provide correct answers and remediation at the end of the quiz.  Have students complete Active Figures 1, 8 & 9.

Students must identify types of plastic pipes and identify fittings and valves for their uses. These tasks correspond to Performance Tasks 1 and 2 respectively.