## Module 02109-05
Carbon Steel Pipe and Fittings

Lesson 1 of 2: Introduction to Carbon Steel Pipe, and Fittings and Valves

This lesson is a classroom session in which the students will learn about carbon steel pipe, fittings, and valves used in modern plumbing systems.  Students will identify the common types of materials, schedules, sizes, and labels used for carbon steel piping, and identify the common fittings and valves used with carbon steel piping to fulfill Performance Task requirements.

Objectives

Upon completion of this lesson, the student should be able to:

- Recognize proper applications of carbon steel piping.

- Describe safety precautions for working with carbon steel piping.

- Identify the material properties, storage, and handling requirements of carbon steel.

- Identify types of fittings used with carbon steel piping.

Performance Requirements

  - Identify the common types of materials, schedules, sizes, and labels used for carbon steel piping. This corresponds to Performance Task 1.

  - Identify the common fittings and valves used with carbon steel piping. This corresponds to Performance Task 2.

Reading Assignment

  - Module 02109, Sections 1 thru 3

Slide Presentation

  - Module 02109, Part 1 (Slides 1 thru 19)

Suggested Equipment/Materials

  - Samples of carbon steel pipe, fittings, and valves used with carbon steel pipe.

Suggested Student Activity

  - Have students visit a construction site where carbon steel piping is being installed.  Have students write a brief report on what they observed.

Testing

  - Module Review Test Questions 1 thru 5 for Sections 2.0.0 - 3.0.0.

  - CONTREN( Connect, Active Figure 9

Suggested Lab Activity

  - Students must identify the common types of materials, schedules, sizes, and labels used for carbon steel piping and identify the common fittings and valves used with carbon steel piping.

Additional Resources

  - Piping Materials Guide, Burlington, MA, Gulf Professional Publishing

  - www.nibco.com/cms.do?id=28pId=104 (Nibco() Information about various kinds of valves

  - Contren Connect Level 1Plumbng Annotated Instructors Guide (available from the NCCER)

SLIDE 1

  - Review the objectives for the module.

  - Review the objectives to be covered in this lesson.  Ask students if they have any questions about the lesson or course objectives.

SLIDE 2

  - Briefly introduce carbon steel piping, including its historical use and the components that it is made of.

SLIDE 3

  - Describe the differences between black steel pipe and galvanized steel pipe.  Have samples of each type available to pass around the class.

  - Explain that to ensure quality, only use pipe that meets ASTM International standards.

  - Describe the characteristics of a standard pipe thread.

  - Explain what “thread engagement” is and how it relates to the proper sealing of a pipe joint.

SLIDE 4

  - Explain that the number of threads per inch and the number of threads needed for sealing vary according to pipe size.

SLIDE 5

  - Describe what is meant by nominal size.

  - Describe the three weights of steel pipe and how weight relates to wall thickness, inside diameter, and outside diameter. See slides 5 & 6 (Figure 2 and Table 3).

  - Describe labeling requirements for steel pipe.

  - Review the storage and handling requirements for steel pipe.

Z

SLIDE 6

No notes

SLIDE 7

  - Describe the difference between pressure fittings and drainage fittings.  Have samples of each type available to pass around the class.

SLIDE 8

  - Describe the purpose of tees in a steel piping system including regular tees (Slide 8, Figure 4) and reducing tees (Slide 9, Figure 5).

  - Have samples of tees available to pass around the class.

SLIDE 9

No notes

SLIDE 10

  - Describe the purpose of elbows in a steel piping system.  Describe the different types of elbows and what they are used for.

  - Have samples of different types of elbows available to pass around the class.

SLIDE 11

  - Describe the purpose of unions in a steel piping system.  Describe and demonstrate how a ground-joint union goes together.

  - Have a ground-joint union available to pass around the class.

SLIDE 12

  - Describe the purpose of flange unions in a steel piping system.  Describe and demonstrate how a flange union goes together.

  - Have a flange union available to pass around the class.

SLIDE 13

  - Describe the purpose of couplings in a steel piping system.

  - Have various couplings available to pass around the class.

.

SLIDE 14

  - Describe the purpose of nipples in a steel piping system.

  - Have a sample of a nipple available to pass around the class.

SLIDE 15

  - Describe the purpose of crosses in a steel piping system.

  - Have a cross available to pass around the class.

SLIDES 16 thru 18

  - Describe the purpose of plugs (Slide 16, Figure 12), caps (Slide 17, Figure 13), and bushings (Slide 18, Figure 14) used in a steel piping system.

  - Have samples of plugs, caps and bushings available to pass around the class.

SLIDE 19

  - Describe the four types of valves (globe, gate, ball, and stop-and waste) used in steel piping systems and explain how each is used are used for.

  - Point out that globe valves are often used for throttling, but that gate valves are not suited for that purpose.

  - Have samples of each type of valve available to pass around the class.

Have students answer Review Questions for Sections 2.0.0 - 3.0.0. Provide correct answers and remediation at the end of the quiz.  Have students complete Active Figure 9.

Students must identify the common types of materials, schedules, sizes, and labels used for carbon steel piping and identify the common fittings and valves used with carbon steel piping. These tasks correspond to Performance Tasks 1 and 2 respectively.