Milling Operations Handout

Name: ____________________________________________________________________________________

Milling Machine Cutting Speeds

High-Speed Steel Cutters                           	Carbide Cutters

Material                       Ft/Min        	M/Min                                  	Ft/Min     	M/Min

Machine steel             	70-100        	21-30                                     	150-250    	45-75

Tool steel                   	60-70         	18-20                                     	125-200     	40-60

Cast iron                     	50-80         	15-25                                     	125-200     	40-60

Bronze                        	65-120        	20-35                                     	200-400    	60-120

Aluminum                  	500-1000    	150-300                               	1000-2000   	300-600

Formula for calculating cutter speeds: 	4 x CS  = R/Min

D

CS- Cutting speed

R/Min- Revolutions per min

Formula for calculating milling feeds: 	N x CPT x (R/Min) = Feed

N- Number of teeth in the milling cutter

CPT- Chip per tooth for a given cutter and metal as shown in the carts above

R/Min- Revolutions per min of the milling cutter

Recommended Feed per Tooth for High Speed Steel Cutters

Slotting                           	Form-

Face          	Helical      	and Side       	End            	Relieved       	Circular

Mills          	Mills          	Mills             	Mills        	Cutters          	Saws

Material        	in./mm      	 in./mm       	in./mm          	in./mm       	in./mm         	in./mm

Aluminum   	 .022/.55      	.018/.45     	.013/.33        	.011/.28       	.007/.18          	.005/.13

Bronze       	 .014/.35    	.011/.28    	.008/.20        	.007/.18      	.004/.10           .003/.08

Cast iron   	 .013/.33      	.010/.25     	.007/.18        	.007/.18      	.004/.10           .003/.08

Machine   	 .012/.30      	.010/.25     	.007/.18        	.006/.15       	.004/.10          	.003/.08

Steel

Tool           	.010/.25     	.008/.20     	.006/.15       	.005/.13       	.003/.08          	.003/.08

Steel

Stainless 	.006/.15     	.005/.13     	.004/.10       	.003/.08       	.002/.05           .002/.05

Steel

Recommended Feed per Tooth for Cemented-Carbide Tipped Cutter

Slotting                           	Form-

Face          	Helical      	and Side       	End            	Relieved        	Circular

Mills          	Mills          	Mills             	Mills           	Cutters           	Saws

Material        	in./mm       	in./mm       	in./mm          	in./mm        	in./mm            	in./mm

Aluminum   	.020/.50      	.016/.40     	.012/.30        	.010/.25       	.006/.15          	.005/.13

Bronze        	.012/.30      	.010/.25     	.007/.18        	.006/.15      	.004/.10           .003/.08

Cast iron    	.016/.40      	.013/.33     	.010/.25        	.008/.20      	.005/.13           .004/.10

Machine    	.016/.40      	.013/.33     	.009/.23        	.008/.20       	.005/.13          	.004/.10

Steel

Tool           	.014/.35      	.011/.28     	.008/.20       	.007/.18       	.004/.10          	.004/.10

Steel

Stainless   	.010/.25     	.008/.20     	.006/.15       	.005/.13       	.003/.08           .003/.08

Steel